Introductory Material Science

Dr. Shih-Hao Lee

Department of Forest Products Science and Furniture Engineering,

National Chiayi University (NCYU)

No.300 Syuefu Rd., Chiayi City 60004, Taiwan (R.O.C.)

Tel: +886-5-2717710; Fax: +886-5-2717497; e-mail: shlee@mail.ncyu.edu.tw

| Course name：Introductory Material Science | Unit： 3 hrs/week：3 |
| --- | --- |
| Year: Sophomore | Course: Required |
| Classroom: | Office Hours: |
| E-mail：shlee@mail.ncyu.edu.tw |  |

A、Course Description：

Introductory Material Science provides broad subjects of the field of material for students who are interested in material. It explores the properties, manufacture and utilization of the traditional material (metals, polymer and ceramics) and advanced material (composite, bio-material and nano-material). The level of this course meets for the students who have learned college chemistry and physics.

At first, atomic structure, inter-atomic bonding, and structure of solid will be introduced and focused on development of student’s ability to visualize how the formation of solid is. After learning the traditional and advanced material, the manufacture and utilization of materials will be discussed.

B、Teaching Goads：

The objectives of this course are to intrigue student’s interests , help student appreciate the underlying logic, help student arrive at answer to any practical problem, and raise ceaseless thought about the potential of material applied in wood products.

It is hoped that this course will enrich the material concepts for those who will not study material further and offer robust and solid foundation for those who study material more intensively and professionally.

C、Class Schedule for the Fall semester in 2010

| Schedule | Topic |
| --- | --- |
| Week 1 | Overviews |
| Week 2 | Atomic structure and inter-atomic bonding. |
| Week 3 | Atomic structure and inter-atomic bonding. |
| Week 4 | The structure of solid |
| Week 5 | The structure of solid |
| Week 6 | Metal |
| Week 7 | Metal |
| Week 8 | Polymer |
| Week 9 | Midterm examination |
| Week 10 | Polymer |
| Week 11 | Ceramic |
| Week 12 | Ceramic |
| Week 13 | Composite |
| Week 14 | Composite |
| Week 15 | Bio-material |
| Week 16 | Nano-material |
| Week 17 | manufacture and utilization of materials |
| Week 18 | Final examination |

D、Grade：

1.  Presence, homeworks or reports  30%	  2. Midterm test  30%	   3. Final test 40%

E、References：

1. William D. Callistr (2002), Materials Science and Engineering an Introduction, John Wiley & Sons, Inc.

2. Thornton Peter A. and Vito J. Colangelo (1985), Fundamentals of Engineering Materials, Prentice-Hall, Inc., Englewood Cliffs, N.J.。

3.Lee, Chun-Ying, Yun-Ming Xy ans Zhong-Ren Chen (1994) Materials Science and Engineering, Gau Li Library Inc.